## Slide 1
POLYMER DENSITY / SAME-TEST-SET COMPARISON
v1 learned polymer density beyond
classical group-contribution estimates
1,077 polymer structures from RadonPy PI1070; the model and physics baseline share the same 216-polymer test set.
Amphora Labs / Confidential / v1 evidence / October 2026
1
Approach
How it was tested
MAE (g/cm3)
Fit (R2)
Van Krevelen physics
Random 60/20/20
train / calibrate / test
0.1327
0.026
Mean baseline
Same test polymers
0.1268
-
Amphora v1 / random forest
646 train / 215 calibrate
216 test
0.0566
0.720
57.3% less error
Learned molecular features improve density estimates over the named physics baseline.
Supports screening within the tested chemical distribution.
Source: RadonPy density comparison receipt [D1]. MD-simulated density at 300 K; random split.
Within-corpus result; novel-chemistry transfer is not established [A1].
Notes: V1 EVIDENCE SLIDES — SOURCE AND SPEAKER NOTES
Prepared 2026-10-16. Presentation styling follows ComparisonSlide.png (white, charcoal, coral highlight).
All charts/tables replot retained v1 results. No new training, experiment, signature verification or lab validation was performed.
SLIDE 1 / DENSITY
MAE 0.1327425203 -> 0.0566447055 g/cm3, a calculated 57.327% reduction.
RadonPy labels are molecular-dynamics simulations, not measured production samples.
Random within-corpus split: 646 train / 215 calibration / 216 test. R2 is not Pearson r.
The source dataset name PI1070 does not determine the retained 1,077-row evaluation count.
SLIDE 2 / THERMAL
Uses the fresh, internally matched C8 comparison: 80.2999166 -> 48.7735715 K MAE, a calculated 39.261% reduction.
265 train / 88 calibration / 89 test = 442 valid experimental OpenPoly records.
The physics baseline was transferred from a simulated Polyuniverse fit without OpenPoly refitting.
This is not a universal win over all physics models or state of the art.
Do not mix this row with the separate 51.2375 K scaffold-LOSO result or its different test protocol.
The final external-validity audit refutes novel-chemistry transfer; these slides preserve a within-corpus claim only.
The Polyuniverse absolute-temperature unit issue is not used as a positive performance claim here.
SLIDE 3 / SOLUBILITY
Full-corpus model RMSE 0.8770255643 vs solvent-mean 1.1686915142 (24.96% reduction).
95% cluster-bootstrap interval 0.8416341721–0.9154344725.
Hardened subset: 94,015 groups / 1,372 solutes; RMSE 0.8741657377 vs 1.1667252776.
517 contradictory state-point groups (1,193 raw rows) excluded from both train/test material.
This is small-molecule solubility supporting formulation research, not polymer dissolution or drug-release validation.
SLIDE 4 / EVIDENCE PROCESS
Density stack same-run RMSE 0.0723218955 vs RF 0.0861986512, but stack MAE 0.0569032315 vs RF 0.0566934387.
This demonstrates why choosing only a flattering metric is insufficient. No blanket claim that physics+ML always wins.
Audit-only development signatures are not external review or scientific validation. No signing-trust claim is made.
Dielectric positive figures from the old pack were omitted because C8 retracts the contaminated-population claim.
Creative license is limited to titles, layout and investment framing. No invented data, scatter points, confidence intervals or competitor results.
SOURCE MAP (repository-relative; SHA256 pins are in source_manifest.json)
D1: v1/amphora-molecule-property/reference/mvp20/data/radonpy_pi1070_density_ml_and_van_krevelen_physics_receipt.v1.json
D2: v1/amphora-molecule-property/reference/mvp20/data/stacked_ml_and_van_krevelen_physics_density_radonpy_receipt.v1.json
T1: v1/amphora-molecule-property/benchmarks/phys-ml-stack-comparison-c8-v3-final/receipt_body.canonical.json
S1: v1/amphora-solvency-score/evidence/audit/hansen-hardened-validation-v1/bigsoldb-admissibility-hardened-lso-receipt.v1.dsse.json
A1: v1/amphora-molecule-property/benchmarks/tg-density-external-validity-c7-v3-final/receipt_body.canonical.json

## Slide 2
THERMAL BEHAVIOR / EXPERIMENTAL POLYMER DATA
v1 benchmarked thermal predictions
against experimental polymer measurements
OpenPoly glass-transition temperature: a matched 89-polymer test set compares physics, learned chemistry and their combination.
Amphora Labs / Confidential / v1 evidence / October 2026
2
Approach
How it was tested
MAE (K)
Fit (R2)
Transferred physics model
Van Krevelen Ridge;
no OpenPoly refitting
80.30
-0.245
Physics + ML stack
Same train / calibrate /
test partition
54.05
0.363
Amphora v1 / random forest
265 train / 88 calibrate
89 test
48.77
0.405
39.3% less error
On this matched test set, learned chemistry outperformed the transferred physics model.
A measured starting point for prioritizing thermal-property experiments.
Source: final physics / ML / stack comparison receipt [T1]. Experimental OpenPoly Tg; fresh random 60/20/20 split.
Baseline was fitted on a different, simulated corpus. Single-corpus benchmark; not prospective lab validation [A1].
Notes: V1 EVIDENCE SLIDES — SOURCE AND SPEAKER NOTES
Prepared 2026-10-16. Presentation styling follows ComparisonSlide.png (white, charcoal, coral highlight).
All charts/tables replot retained v1 results. No new training, experiment, signature verification or lab validation was performed.
SLIDE 1 / DENSITY
MAE 0.1327425203 -> 0.0566447055 g/cm3, a calculated 57.327% reduction.
RadonPy labels are molecular-dynamics simulations, not measured production samples.
Random within-corpus split: 646 train / 215 calibration / 216 test. R2 is not Pearson r.
The source dataset name PI1070 does not determine the retained 1,077-row evaluation count.
SLIDE 2 / THERMAL
Uses the fresh, internally matched C8 comparison: 80.2999166 -> 48.7735715 K MAE, a calculated 39.261% reduction.
265 train / 88 calibration / 89 test = 442 valid experimental OpenPoly records.
The physics baseline was transferred from a simulated Polyuniverse fit without OpenPoly refitting.
This is not a universal win over all physics models or state of the art.
Do not mix this row with the separate 51.2375 K scaffold-LOSO result or its different test protocol.
The final external-validity audit refutes novel-chemistry transfer; these slides preserve a within-corpus claim only.
The Polyuniverse absolute-temperature unit issue is not used as a positive performance claim here.
SLIDE 3 / SOLUBILITY
Full-corpus model RMSE 0.8770255643 vs solvent-mean 1.1686915142 (24.96% reduction).
95% cluster-bootstrap interval 0.8416341721–0.9154344725.
Hardened subset: 94,015 groups / 1,372 solutes; RMSE 0.8741657377 vs 1.1667252776.
517 contradictory state-point groups (1,193 raw rows) excluded from both train/test material.
This is small-molecule solubility supporting formulation research, not polymer dissolution or drug-release validation.
SLIDE 4 / EVIDENCE PROCESS
Density stack same-run RMSE 0.0723218955 vs RF 0.0861986512, but stack MAE 0.0569032315 vs RF 0.0566934387.
This demonstrates why choosing only a flattering metric is insufficient. No blanket claim that physics+ML always wins.
Audit-only development signatures are not external review or scientific validation. No signing-trust claim is made.
Dielectric positive figures from the old pack were omitted because C8 retracts the contaminated-population claim.
Creative license is limited to titles, layout and investment framing. No invented data, scatter points, confidence intervals or competitor results.
SOURCE MAP (repository-relative; SHA256 pins are in source_manifest.json)
D1: v1/amphora-molecule-property/reference/mvp20/data/radonpy_pi1070_density_ml_and_van_krevelen_physics_receipt.v1.json
D2: v1/amphora-molecule-property/reference/mvp20/data/stacked_ml_and_van_krevelen_physics_density_radonpy_receipt.v1.json
T1: v1/amphora-molecule-property/benchmarks/phys-ml-stack-comparison-c8-v3-final/receipt_body.canonical.json
S1: v1/amphora-solvency-score/evidence/audit/hansen-hardened-validation-v1/bigsoldb-admissibility-hardened-lso-receipt.v1.dsse.json
A1: v1/amphora-molecule-property/benchmarks/tg-density-external-validity-c7-v3-final/receipt_body.canonical.json

## Slide 3
FORMULATION SUPPORT / UNSEEN-SOLUTE TESTING
v1 improved solubility predictions
for molecules withheld from training
BigSolDB: 94,532 measurement groups across 1,372 solutes, evaluated with leave-solute-out cross-validation.
Amphora Labs / Confidential / v1 evidence / October 2026
3
Approach
How it was tested
RMSE (log S)
Best naive baseline
Solvent-mean baseline
on the same evaluation
1.169
Data-cleaning stress test
Contradictory state-point
groups removed; same protocol
0.874
Amphora v1
Test solutes withheld
from training
0.877
25.0% less error
The advantage held after removing contradictory measurements: RMSE 0.877 became 0.874.
Relevant to solvent selection; this is not a drug-release benchmark.
Source: BigSolDB admissibility-hardened leave-solute-out audit [S1]. Full-corpus RMSE 95% CI: 0.842-0.915.
Literature-data benchmark and internal robustness audit; no prospective formulation or release claim.
Notes: V1 EVIDENCE SLIDES — SOURCE AND SPEAKER NOTES
Prepared 2026-10-16. Presentation styling follows ComparisonSlide.png (white, charcoal, coral highlight).
All charts/tables replot retained v1 results. No new training, experiment, signature verification or lab validation was performed.
SLIDE 1 / DENSITY
MAE 0.1327425203 -> 0.0566447055 g/cm3, a calculated 57.327% reduction.
RadonPy labels are molecular-dynamics simulations, not measured production samples.
Random within-corpus split: 646 train / 215 calibration / 216 test. R2 is not Pearson r.
The source dataset name PI1070 does not determine the retained 1,077-row evaluation count.
SLIDE 2 / THERMAL
Uses the fresh, internally matched C8 comparison: 80.2999166 -> 48.7735715 K MAE, a calculated 39.261% reduction.
265 train / 88 calibration / 89 test = 442 valid experimental OpenPoly records.
The physics baseline was transferred from a simulated Polyuniverse fit without OpenPoly refitting.
This is not a universal win over all physics models or state of the art.
Do not mix this row with the separate 51.2375 K scaffold-LOSO result or its different test protocol.
The final external-validity audit refutes novel-chemistry transfer; these slides preserve a within-corpus claim only.
The Polyuniverse absolute-temperature unit issue is not used as a positive performance claim here.
SLIDE 3 / SOLUBILITY
Full-corpus model RMSE 0.8770255643 vs solvent-mean 1.1686915142 (24.96% reduction).
95% cluster-bootstrap interval 0.8416341721–0.9154344725.
Hardened subset: 94,015 groups / 1,372 solutes; RMSE 0.8741657377 vs 1.1667252776.
517 contradictory state-point groups (1,193 raw rows) excluded from both train/test material.
This is small-molecule solubility supporting formulation research, not polymer dissolution or drug-release validation.
SLIDE 4 / EVIDENCE PROCESS
Density stack same-run RMSE 0.0723218955 vs RF 0.0861986512, but stack MAE 0.0569032315 vs RF 0.0566934387.
This demonstrates why choosing only a flattering metric is insufficient. No blanket claim that physics+ML always wins.
Audit-only development signatures are not external review or scientific validation. No signing-trust claim is made.
Dielectric positive figures from the old pack were omitted because C8 retracts the contaminated-population claim.
Creative license is limited to titles, layout and investment framing. No invented data, scatter points, confidence intervals or competitor results.
SOURCE MAP (repository-relative; SHA256 pins are in source_manifest.json)
D1: v1/amphora-molecule-property/reference/mvp20/data/radonpy_pi1070_density_ml_and_van_krevelen_physics_receipt.v1.json
D2: v1/amphora-molecule-property/reference/mvp20/data/stacked_ml_and_van_krevelen_physics_density_radonpy_receipt.v1.json
T1: v1/amphora-molecule-property/benchmarks/phys-ml-stack-comparison-c8-v3-final/receipt_body.canonical.json
S1: v1/amphora-solvency-score/evidence/audit/hansen-hardened-validation-v1/bigsoldb-admissibility-hardened-lso-receipt.v1.dsse.json
A1: v1/amphora-molecule-property/benchmarks/tg-density-external-validity-c7-v3-final/receipt_body.canonical.json

## Slide 4
EVIDENCE PROCESS / REPEATABLE TECHNICAL DILIGENCE
v1 built an evidence trail
behind the performance numbers
Named baselines, retained test protocols and explicit failure findings make the results inspectable.
Amphora Labs / Confidential / v1 evidence / October 2026
4
01
Compare fairly
Density and thermal comparisons use matched test sets. Solubility holds entire solutes out of training.
02
Challenge the data
Removing contradictory solubility measurements preserved the gain: RMSE 0.877 to 0.874.
03
Keep the failures
Hybrid density improved RMSE, but not MAE. Novel-chemistry transfer failed; its limits remain explicit.
The investment case: an existing, inspectable foundation for choosing the next experiments.
Sources: comparison receipts [D1, T1], solubility stress test [S1], density stack [D2], external-validity audit [A1].
Retrospective computational evidence. Source receipts retain their original audit status; signatures were not re-verified for this deck.
Notes: V1 EVIDENCE SLIDES — SOURCE AND SPEAKER NOTES
Prepared 2026-10-16. Presentation styling follows ComparisonSlide.png (white, charcoal, coral highlight).
All charts/tables replot retained v1 results. No new training, experiment, signature verification or lab validation was performed.
SLIDE 1 / DENSITY
MAE 0.1327425203 -> 0.0566447055 g/cm3, a calculated 57.327% reduction.
RadonPy labels are molecular-dynamics simulations, not measured production samples.
Random within-corpus split: 646 train / 215 calibration / 216 test. R2 is not Pearson r.
The source dataset name PI1070 does not determine the retained 1,077-row evaluation count.
SLIDE 2 / THERMAL
Uses the fresh, internally matched C8 comparison: 80.2999166 -> 48.7735715 K MAE, a calculated 39.261% reduction.
265 train / 88 calibration / 89 test = 442 valid experimental OpenPoly records.
The physics baseline was transferred from a simulated Polyuniverse fit without OpenPoly refitting.
This is not a universal win over all physics models or state of the art.
Do not mix this row with the separate 51.2375 K scaffold-LOSO result or its different test protocol.
The final external-validity audit refutes novel-chemistry transfer; these slides preserve a within-corpus claim only.
The Polyuniverse absolute-temperature unit issue is not used as a positive performance claim here.
SLIDE 3 / SOLUBILITY
Full-corpus model RMSE 0.8770255643 vs solvent-mean 1.1686915142 (24.96% reduction).
95% cluster-bootstrap interval 0.8416341721–0.9154344725.
Hardened subset: 94,015 groups / 1,372 solutes; RMSE 0.8741657377 vs 1.1667252776.
517 contradictory state-point groups (1,193 raw rows) excluded from both train/test material.
This is small-molecule solubility supporting formulation research, not polymer dissolution or drug-release validation.
SLIDE 4 / EVIDENCE PROCESS
Density stack same-run RMSE 0.0723218955 vs RF 0.0861986512, but stack MAE 0.0569032315 vs RF 0.0566934387.
This demonstrates why choosing only a flattering metric is insufficient. No blanket claim that physics+ML always wins.
Audit-only development signatures are not external review or scientific validation. No signing-trust claim is made.
Dielectric positive figures from the old pack were omitted because C8 retracts the contaminated-population claim.
Creative license is limited to titles, layout and investment framing. No invented data, scatter points, confidence intervals or competitor results.
SOURCE MAP (repository-relative; SHA256 pins are in source_manifest.json)
D1: v1/amphora-molecule-property/reference/mvp20/data/radonpy_pi1070_density_ml_and_van_krevelen_physics_receipt.v1.json
D2: v1/amphora-molecule-property/reference/mvp20/data/stacked_ml_and_van_krevelen_physics_density_radonpy_receipt.v1.json
T1: v1/amphora-molecule-property/benchmarks/phys-ml-stack-comparison-c8-v3-final/receipt_body.canonical.json
S1: v1/amphora-solvency-score/evidence/audit/hansen-hardened-validation-v1/bigsoldb-admissibility-hardened-lso-receipt.v1.dsse.json
A1: v1/amphora-molecule-property/benchmarks/tg-density-external-validity-c7-v3-final/receipt_body.canonical.json