TEST PROTOCOL AND STATEMENT OF WORK

Two-Component Epoxy-Polyamide Marine Hull Primer — Validation Campaign 001

| Protocol No. / Rev | AMP-CRO-001 / Rev A (draft for CRO review and quotation) |
| --- | --- |
| Sponsor | Amphora Bio, Inc. — Technical contact: [name, e-mail, phone] |
| Test articles | Formulation AMP-EP-0001 and variants (Section 2). Sponsor supplies raw materials with lot CoAs, batch instructions, and mixing/application datasheet. CRO manufactures paint at bench scale per Section 3. |
| Reference class | MIL-DTL-24441-class performance methods. This campaign is a screening/validation program, NOT a QPL qualification submission. |
| Duration | Week-1 liquid data → 1,000 h screening read (~20 weeks); optional 3,000 h qualification arm continues to ~week 40. Stability arm runs in parallel. |
| Quotation basis | ~14 paint systems/variants, ~90–110 coated panels plus retains, methods and timepoints per Sections 3–7. |

# 1. Purpose

Generate measured liquid-paint, application, cured-film, corrosion/immersion, and stability data for a computationally designed epoxy-polyamide hull primer, side-by-side against a commercial qualified control and a pigment-free null coating. All acceptance targets and rankings are pre-registered by the Sponsor before exposure begins; the CRO's role is execution, measurement, and raw-data return. The Sponsor's analysis pipeline requires raw instrument files — summary-only reporting does not fulfill this contract (Section 8).

# 2. Test Systems

| System ID | Description | Role |
| --- | --- | --- |
| V0 | AMP-EP-0001 nominal (0.98:1 amine:epoxy) | Primary candidate |
| V3 / V4 | Polyamide +5% (1.03:1) / −5% (0.93:1) | Stoichiometry bracket |
| V1 / V2 | Solvent −8% / +8% | Application/spray window arm only |
| V5 | Flatting silica +50% | Sheen arm only |
| E65 | Zinc-phosphate variant (Sponsor recipe) | Inhibitor comparison |
| L60 | 60% volume-solids lineage benchmark (Sponsor recipe) | Benchmark |
| PC | Commercial QPL-24441-qualified primer, CRO-purchased, lot recorded | Positive control |
| NULL | Pigment-free epoxy-polyamide clear at equal DFT (Sponsor recipe) | Negative/null control |
| BLANK | Uncoated blasted steel | Substrate baseline |

Substrate: carbon-steel panels, abrasive-blasted to SSPC-SP 10/NACE No. 2 near-white, 2.5–3.5 mil angular profile verified by replica tape (ASTM D4417 Method C). Replication: minimum n = 3 panels per system per exposure arm, plus 2 retained panels per system, archived uncoated-edge-sealed. Every panel serialized; photographed before coating, after coating, and at every inspection.

# 3. Phase 1 — Paint Manufacture and Liquid-Paint Testing (Week 1)

| ID | Task and method | Systems | Target / endpoint | Required data deliverable |
| --- | --- | --- | --- | --- |
| 1.1 | Manufacture Components A and B per Sponsor batch instructions; record all charge weights, disperser tip speeds, times, temperatures. Grind per ASTM D1210: Component A to Hegman ≥ 6; Component B to Hegman ≥ 4. | V0–V5, E65, L60, NULL | Grind endpoints met; full batch record | Complete batch record per batch (Sponsor template) |
| 1.2 | In-process QC on each component: density ASTM D1475; nonvolatile ASTM D2369; Stormer viscosity ASTM D562. | All manufactured | Density within ±0.02 g/mL and NV within ±1% of Sponsor theoretical values (provided per system) | Numeric results + instrument printouts; flag any out-of-window result before proceeding |
| 1.3 | Mixed-paint verification at 1:1 by volume after 30-min induction: volume solids ASTM D2697; VOC EPA Method 24; weight per gallon ASTM D1475. | V0, V3, V4, E65, L60 | VS 65 ± 2% (L60: 60.2 ± 2%); VOC ≤ 340 g/L; WPG ~9.1–9.2 lb/gal | Raw worksheets + results per system |
| 1.4 | Pot life: 30-min induction, then Stormer KU (D562) every 15 min at 65°F, 73°F/50% RH, and 95°F until endpoint (25 KU rise over initial, or viscosity doubling). | V0, V3, V4 | Report full KU-vs-time curve at each temperature; envelope target ≥ 1.5 h at 73°F | Time-stamped KU log (CSV) per system per temperature — 9 curves total |
| 1.5 | Drying times ASTM D5895 (dry-to-touch, dry-hard) at 73°F/50% RH; practical recoat check: second coat at 6 h + intercoat adhesion by D3359 or D4541 after 7-day cure. | V0, V3, V4 | DTT ~2 h; recoat at ~6 h without intercoat failure | Drying recorder trace + recoat adhesion results |
| 1.6 | Application trial: airless spray to 7–9 mil WFT on vertical panels; record WFT/DFT pairs, sag per ASTM D4400 (anti-sag index), pinholing, flow-out. Repeat with V1/V2 to bracket spray solids. | V0–V5 | 4.5–6.0 mil DFT per coat without sagging at 9 mil WFT | WFT/DFT table, D4400 rating, application notes, panel photos |

# 4. Phase 2 — Cured-Film Properties (Weeks 2–4)

| ID | Task and method | Systems | Target / endpoint | Required data deliverable |
| --- | --- | --- | --- | --- |
| 2.1 | DFT mapping per SSPC-PA 2 using ASTM D7091 gauges; 5 spots per panel, all exposure panels. | All coated | 4.5–6.0 mils/coat | Per-panel DFT map keyed to panel serial |
| 2.2 | Specular gloss ASTM D523 at 60°, 7-day cure. | V0, V5 | Low-sheen; V5 establishes silica-loading slope | Gloss readings, 3 per panel |
| 2.3 | Pull-off adhesion ASTM D4541 (Type V self-aligning), 7-day cure, dry film. | All incl. PC, NULL | Report value + failure mode (adhesive/cohesive/glue); working floor 500 psi | Per-dolly value, failure-mode photo |

# 5. Phase 3 — Corrosion and Immersion (Weeks 2–20; qualification arm to week 40)

Rank lock: before any panel enters a chamber, the Sponsor files a sealed predicted performance ranking of {V0, V3, V4, E65, L60, NULL}. The CRO acknowledges receipt in writing. No re-ranking after exposure begins. The CRO is not asked to evaluate the prediction — only to measure and rate blind to it.

| ID | Task and method | Systems | Target / endpoint | Required data deliverable |
| --- | --- | --- | --- | --- |
| 3.1 | Salt fog ASTM B117. Scribed panels (50 mm vertical scribe to substrate per D1654 practice). Pulls at 250 / 500 / 1,000 h; screening decision at 1,000 h; continue n=3 subset to 3,000 h (qualification arm, Sponsor option). Rate scribe creep per D1654 Procedure A and blistering per D714 at each pull. | All systems + PC, NULL; n=3 per pull schedule | Screening: candidate within 1 rating unit of PC at 1,000 h | D1654/D714 ratings per panel per timepoint; high-res photos at every pull; chamber log (temp, collection rate, pH, salinity) |
| 3.2 | Cyclic corrosion ASTM D5894, 8 cycles (~2,688 h): alternating fluorescent UV/condensation (G154) and salt-fog/dry (G85 A5 prohesion). Same scribe/rating scheme and pull cadence per cycle. | V0, E65, L60, PC | Comparative rank vs B117 arm | Same rating/photo package per cycle |
| 3.3 | Immersion ASTM D870 in synthetic seawater (ASTM D1141), 73°F. Inspections at 30 and 90 days: blistering D714, visual defects, plus wet-recovery pull-off adhesion D4541 at 90 days (24 h recovery). | All systems + PC, NULL; n=3 | No blistering at 30 d; 90-d adhesion ≥ 70% of dry value | Ratings, photos, adhesion values + failure modes |
| 3.4 | EIS per ISO 16773 parts 2–4: immersed-cell setup on dedicated unscribed panels in D1141 seawater; 100 kHz → 0.01 Hz, 10 mV RMS vs OCP; timepoints 0 (24 h wet-in), 7 d, 30 d, 90 d. | V0, V3, V4, E65, NULL, PC; n=3 cells | Track ¦Z¦ at 0.01 Hz over time; no acceptance bar — measurement arm | FULL raw spectra as CSV (frequency, Z-real, Z-imag) per cell per timepoint + cell photos; no fitted-only summaries |

# 6. Phase 4 — Package Stability and Raw-Material Verification (starts Week 1, parallel)

| ID | Task and method | Systems | Target / endpoint | Required data deliverable |
| --- | --- | --- | --- | --- |
| 4.1 | Accelerated storage: seal Components A and B separately, 4 weeks at 120°F. Weekly: viscosity D562, settling D869. After aging: repeat mixed-paint tests 1.3, 1.4 (73°F only), 1.5. | V0 components | ≤ 10 KU drift; settling rating ≥ 6; aged mix re-passes 1.3 | Weekly logs + post-age retest results |
| 4.2 | Raw-material verification on the actual lots used: epoxide equivalent weight by ASTM D1652; amine value by ASTM D2074 (or titrated AHEW per Sponsor method). | Epoxy + polyamide lots | Report measured values; Sponsor recomputes mix ratios and confirms in writing before Phase 1 mixing | Titration raw data + certificates; HOLD POINT: do not mix until Sponsor confirms |

# 7. Inspection and Reporting Schedule

- Week 1: batch records, 1.2–1.6 results, 4.2 hold-point data — within 5 business days of completion.

- Weeks 2–4: Phase 2 package.

- Exposure pulls: ratings + photos within 3 business days of each pull (250/500/1,000 h B117; per-cycle D5894; 30/90-d immersion; each EIS timepoint).

- Screening report: consolidated data package at 1,000 h B117 + 90-d immersion (~week 20).

- Qualification arm (option): 3,000-h B117 continuation report ~week 40.

# 8. Data Return, Custody, and Deviations (contract-critical)

- Raw files are the deliverable. Instrument exports (KU logs, EIS spectra, gloss, adhesion gauge), calibration certificates for every instrument used, chamber environment logs, and serialized panel photos at every inspection. PDF summaries alone are non-conforming.

- Chain of custody: every sample, panel, and datum keyed to system ID, batch record, and panel serial. Sponsor provides ID scheme and file-naming/format template (raw-data acceptance schema) in the handoff packet; CRO returns data in that structure.

- Controls travel with candidates: candidate and control panels share chambers, racks, and rating sessions. A candidate datum without its same-session control datum will be rejected by Sponsor intake.

- Deviations: any departure from this protocol (temperature excursion, missed pull, panel damage) is reported as a written deviation record within 2 business days, with affected panel serials. Deviations do not void data — unreported deviations do.

- Retains: retain samples of each liquid batch (500 mL A + B) and 2 unexposed panels per system for 12 months.

- Blind rating: panels are rated by system ID code only; the CRO rating technician is not shown Sponsor predictions or formulation identities beyond the ID code.

# 9. Sponsor-Supplied Items

- Raw materials with lot CoAs (or CRO purchases against Sponsor-specified grades; lots recorded either way).

- Batch instructions, mixing/application datasheet, theoretical QC values per system, panel ID scheme, and the raw-data acceptance schema/templates.

- Sealed predicted-ranking envelope (Section 5) and written confirmation at the 4.2 hold point.

# 10. Acceptance of This Protocol

CRO review is invited on method substitutions (e.g., equivalent drying recorder, EIS cell geometry), panel counts, and schedule. Substitutions require written Sponsor approval and become Rev B of this protocol before work begins.

| Sponsor — name / signature / date | CRO — name / signature / date |
| --- | --- |