AMPHORA  ·  MATERIALS FORMULATION PLATFORM

Two-Component Epoxy-Polyamide Marine Hull Primer

Formulation White Paper & CRO Handoff Basis — AMP-EP-0001 (Black)

Customer: a top U.S. Navy prime (masked)   ·   Version 1.0   ·   July 5, 2026   ·   Status: engine-verified, pending wet-lab validation

# 1. Executive Summary

This white paper delivers a complete, auditable starting-point formulation for the two-component, solvent-borne epoxy-polyamide marine hull primer defined by the customer technical envelope ("Jepson Technical Envelope") and its companion Self-Directed Formulation Charter. The formulation was designed from first principles and verified computationally on the Amphora materials formulation platform, whose physics engine computes volume solids, VOC (EPA Method 24 convention), density, pigment volume concentration (PVC), critical PVC, film-build, coverage, and cost directly from composition.

The candidate formulation, AMP-EP-0001, satisfies every fixed constraint of the envelope simultaneously: 65.0% volume solids (target 65% ± 2%), VOC 298 g/L (limit ≤ 340 g/L), 9.17 lb/gal (target ~9.1), 1:1 mix ratio by volume with a 0.98:1 amine:epoxy stoichiometric ratio, dry film build of 4.55–5.85 mils per coat from the specified 7.0–9.0 mil wet film (target 4.5–6.0), and theoretical coverage of 178–229 ft²/gal (target 175–230). PVC of 10.3% sits far below the computed CPVC of 40.3%, consistent with a dense, continuous barrier film for immersion service, and with the envelope’s stipulation that pigmentation is non-functional (identification/visibility only). Modeled raw-material cost is $2.75/kg ($3.03/L).

All computed values are model outputs from declared raw-material properties, not measurements. Per the charter’s auditability mandate, every material choice carries a stated rationale and confidence rating (Section 9), and Section 8 provides the bench validation plan a CRO can execute to qualify the system against the envelope and MIL-DTL-24441-class performance requirements. Results returned from that work feed Amphora’s Bayesian optimization loop to refine subsequent iterations.

# 2. Inputs and Mandate

Two seed documents constitute the sole problem statement, per the charter’s zero-prior operating principle:

- Jepson Technical Envelope — the binding product definition: two-component epoxy-polyamide chemistry, 1:1 by volume, solvent-borne, ~65% volume solids (±2%), VOC ≤ 340 g/L, DFT 4.5–6.0 mils/coat, recoat ~6 h, shelf life ~36 months, immersion service on abrasive-blasted carbon steel (near-white, 2.5–3.5 mil profile), low sheen, black and yellow identification colors.

- Self-Directed Formulation Charter — objectives and guardrails: the deliverable must be cited, CRO-executable, human-interpretable, confidence-rated, and validation-backed, with discoveries quarantined to a separate annex and the customer masked throughout.

This paper is the formulation core of the required deliverable set. Manufacturing process, QC, and validation are outlined at handoff depth (Sections 6–8); full production-scale process engineering, supply-chain, regulatory, and IP work packages are scoped but deferred to the program’s next phase.

# 3. Methodology — the Amphora Engine

Amphora is a formulation R&D platform whose core is a stateless coating-physics engine and a Gaussian-process suggestion engine. For this program the workflow was: (1) derive the design logic for an epoxy-polyamide immersion primer from first principles and the constraints in the envelope; (2) encode candidate raw materials with their physical constants (density, nonvolatile fraction, oil absorption, cost); (3) solve the composition analytically against the binding constraints; (4) verify the composition on the engine; and (5) probe the formulation’s sensitivity with an engine-verified variant ladder that doubles as the CRO screening DOE.

Models used, all standard coatings-industry calculations executed by the engine: ideal-mixing wet density, ρ = 1/Σ(wᵢ/ρᵢ); solids by weight and volume; PVC as pigment-plus-extender dry volume over total dry volume; CPVC from oil absorption (linseed-oil model); VOC per EPA Method 24 convention (grams volatile organic per liter of coating; no water or exempt solvents are present in this solvent-borne system); film build DFT = WFT × volume solids; theoretical coverage = 1604 × volume solids / DFT(mils) ft²/gal; and mass-weighted raw-material cost. Cure kinetics (pot life, dry-to-touch, recoat) are not first-principles outputs of the current engine; they are addressed by material selection, use-level rationale, and the bench plan.

# 4. Design Rationale

## 4.1 Binder system and stoichiometry

The envelope fixes the chemistry: ambient-cure epoxy-polyamide. A standard liquid bisphenol-A diglycidyl ether (DGEBA) epoxy resin, EEW 182–192 g/eq (e.g., the EPON 828 / D.E.R. 331 / YD-128 class), is selected as the epoxy backbone: it is 100% solids (helping the 65% volume-solids target at legal VOC), universally available from multiple domestic suppliers, and the reference resin for MIL-DTL-24441-class systems. The curative is a reactive polyamide of amine value 230–246 mg KOH/g (the Versamid 115 / Ancamide 220 class), chosen over faster amine adducts because polyamides deliver the long pot life, forgiving surface wetting, water/salt resistance, and flexibility on blast-profiled steel that immersion service demands — at the cost of the ~30 min induction the envelope already accommodates.

Stoichiometry: 27.0 parts epoxy (EEW 190 → 0.1421 eq) to 16.0 parts polyamide (AHEW ≈ 115 → 0.1391 eq) gives an amine:epoxy ratio of 0.98:1 — essentially stoichiometric, slightly amine-lean, which favors full epoxy conversion and water resistance. Polyamide AHEW is nominal and batch-dependent; the ratio must be recomputed from the supplier certificate of analysis at the bench (Section 9). The ±5% curative ladder variants V3/V4 bracket this uncertainty.

## 4.2 Pigmentation philosophy — low PVC barrier film

The envelope states pigmentation is non-functional (identification only), and the ~9.1 lb/gal weight-per-gallon target independently rules out a heavily extended film: at 65% volume solids, high pigment loadings push density well above 10 lb/gal. Both signals point to a binder-rich barrier primer. AMP-EP-0001 therefore carries a PVC of 10.3% against a computed CPVC of 40.3% — a large formulating margin that ensures a dense, pore-free film whose corrosion protection derives from the crosslinked epoxy matrix and its adhesion to the blast profile rather than from active pigments. Color is delivered by 1.0 wt% carbon black (black variant); the yellow variant substitutes ~3 wt% rutile TiO2 plus ~2 wt% inorganic yellow iron oxide with a compensating talc reduction, and must be re-verified on the engine before release (one preview call).

Platy talc (10.4 wt%) provides film reinforcement, intercoat adhesion, and mild barrier-tortuosity benefits at low cost; a small charge of untreated flatting silica (3.9 wt%) knocks the 60° sheen down to the specified low-sheen finish without meaningfully raising PVC. Both are inert in immersion.

## 4.3 Solvent system and VOC positioning

A 75:25 (by mass) xylene : n-butanol blend is the classic epoxy-polyamide vehicle: xylene cuts both resins efficiently; n-butanol suppresses polyamide hydrogen-bonded gelation, improves flow-out and pot-life stability, and moderates flash-off for airless spray at 7–9 mil WFT. Total solvent is solved analytically so mixed volume solids lands exactly on 65.0%, which places VOC at 298 g/L — a 42 g/L compliance margin under the 340 g/L ceiling that absorbs bench-stage thinning adjustments (each +8% solvent adds ~15 g/L; see ladder V2). The engine’s advisory flag at 250 g/L reflects architectural limits and is not applicable to this industrial-maintenance category.

## 4.4 Rheology and package split

Organoclay (0.9 wt% mixed basis, split between components and activated during each grind) provides anti-settling and the sag resistance needed to hold 9 mil WFT on vertical hull plate. The 1:1 volume split is engineered by placing the epoxy resin, carbon black, and liquid additives in Component A (70.2% volume solids) and the polyamide with the talc/silica extender grind in Component B (59.8% volume solids) — polyamides are effective pigment-wetting vehicles, and pigmenting B keeps A’s viscosity manageable without extra solvent. Each component is independently shelf-stable; the 36-month target is addressed in QC (Section 7) and validation (Section 8).

# 5. Formulation — AMP-EP-0001

## 5.1 Mixed-system composition (A + B combined at 1:1 by volume)

| Raw material (grade/spec attribute) | Function | Wt % (mixed) | ρ, g/mL | NV fraction | Candidate sources |
| --- | --- | --- | --- | --- | --- |
| DGEBA liquid epoxy resin, EEW 182–192 | Binder (A) | 35.03 | 1.16 | 1.00 | Westlake, Olin, Kukdo |
| Polyamide resin, AV 230–246, AHEW ~115 | Curative (B) | 20.76 | 0.97 | 1.00 | Gabriel, BASF, Evonik |
| Xylene, mixed isomers | Solvent | 20.32 | 0.865 | 0 | Multiple domestic |
| Talc, platy Mg-silicate, 325 mesh | Extender (B) | 10.38 | 2.75 | 1.00 | Imerys, Barretts |
| n-Butanol | Co-solvent | 6.77 | 0.81 | 0 | Multiple domestic |
| Flatting silica, untreated, ~5 µm | Matting (B) | 3.89 | 2.20 | 1.00 | Evonik, PPG |
| Carbon black, medium color | ID pigment (A) | 1.04 | 1.80 | 1.00 | Cabot, Birla |
| Organoclay rheology modifier | Anti-sag/settle | 0.91 | 1.70 | 1.00 | BYK, Elementis |
| Dispersant / wetting additive | Pigment wetting (A) | 0.52 | 1.00 | 1.00* | BYK, Lubrizol |
| Defoamer / flow additive | Film quality (A) | 0.39 | 1.00 | 1.00* | BYK, Evonik |

* Additives modeled at 100% NV for simplicity; actual carriers are counted against the VOC margin at the bench (see Section 9). Total = 100.00 wt%.

## 5.2 Component A — epoxy grind (per 100 g of A)

| Raw material | Wt % of Component A |
| --- | --- |
| DGEBA liquid epoxy resin | 71.54 |
| Xylene | 17.66 |
| n-Butanol | 5.89 |
| Carbon black | 2.12 |
| Dispersant / wetting additive | 1.06 |
| Organoclay | 0.93 |
| Defoamer / flow additive | 0.79 |

Component A: 70.2% volume solids; supplied as the pigmented epoxy base.

## 5.3 Component B — polyamide grind (per 100 g of B)

| Raw material | Wt % of Component B |
| --- | --- |
| Polyamide resin (AV 230–246) | 40.67 |
| Xylene | 22.87 |
| Talc, 325 mesh | 20.33 |
| Flatting silica | 7.62 |
| n-Butanol | 7.62 |
| Organoclay | 0.89 |

Component B: 59.8% volume solids. Mix A:B = 1:1 by volume; 30 min induction (sweat-in) at ≥60°F material temperature before application, per envelope.

# 6. Engine-Computed Properties vs. Envelope

All values below were computed by the Amphora physics engine from the composition in Section 5 (formulation record AMP-EP-0001), except rows marked "derived," which follow arithmetically from engine outputs.

| Property | Envelope requirement | AMP-EP-0001 | Basis | Status |
| --- | --- | --- | --- | --- |
| Volume solids | ~65% (±2%) | 65.0% | engine | PASS |
| VOC (Method 24 conv.) | ≤340 g/L | 298 g/L | engine | PASS |
| Weight per gallon | ~9.1 lb/gal | 9.17 lb/gal (ρ 1.099) | engine | PASS |
| Mix ratio | 1:1 by volume | 1:1 by volume | design | PASS |
| Amine:epoxy stoichiometry | sound chemistry | 0.98 : 1 | design | PASS |
| DFT per coat @ 7–9 mil WFT | 4.5–6.0 mils | 4.55–5.85 mils | derived | PASS |
| Coverage | 175–230 ft²/gal | 178–229 ft²/gal | derived | PASS |
| PVC vs CPVC | continuous barrier film | 10.3% vs 40.3% | engine | PASS |
| Solids by weight | — | 72.9% | engine | info |
| Raw material cost | — | $2.75/kg · $3.03/L | engine | info |

Pot life (≥1.5 h), induction (~30 min), dry-to-touch (~2 h), recoat (~6 h), functional cure (~6 h), and 36-month shelf life are properties of cure kinetics and package stability that the current engine does not predict from first principles. The selected polyamide class and use level are the industry-standard route to exactly this cure profile, but these five parameters are bench-verification items (Section 8) and carry medium confidence until measured.

# 7. Engine-Verified Variant Ladder (CRO Screening DOE)

Six compositions were run through the engine to bracket the principal formulation risks: solvent demand at spray viscosity (V1/V2), curative stoichiometry against CoA variation (V3/V4), and sheen (V5). Every variant remains inside the envelope, meaning the CRO can screen the full ladder without leaving the compliance window.

| Variant | Vol. solids % | VOC g/L | lb/gal | PVC % | Cost $/kg |
| --- | --- | --- | --- | --- | --- |
| V0 — nominal | 65.0 | 298 | 9.17 | 10.3 | 2.75 |
| V1 — solvent −8% | 66.9 | 282 | 9.23 | 10.3 | 2.79 |
| V2 — solvent +8% | 63.2 | 313 | 9.11 | 10.3 | 2.72 |
| V3 — polyamide +5% (1.03:1) | 65.4 | 294 | 9.16 | 10.2 | 2.77 |
| V4 — polyamide −5% (0.93:1) | 64.6 | 301 | 9.18 | 10.5 | 2.73 |
| V5 — flatting silica +50% | 65.3 | 295 | 9.26 | 11.7 | 2.76 |

Recommended bench sequence: prepare V0, V3, V4 first (stoichiometry is the dominant film-property variable), select the best cure/film balance, then tune spray solids with V1/V2 and sheen with V5. Each result logged against the Amphora formulation record enables the platform’s Gaussian-process optimizer to propose the next round once ≥5 measured points exist for a given objective (e.g., 60° gloss, pull-off adhesion, or salt-fog creep).

# 8. Manufacturing Outline, QC, and Validation Plan

## 8.1 Bench / pilot process

- Component A: charge epoxy resin + 80% of A-solvent; disperse organoclay to full activation (high-speed disperser, ~18–20 m/s tip speed, 15 min); add dispersant, then carbon black; grind to ≤ 25 µm (Hegman ≥ 6, ASTM D1210) on the HSD or a bead mill; let down with defoamer and remaining solvent.

- Component B: charge polyamide + 80% of B-solvent; activate organoclay; add talc then silica under high shear; grind to ≤ 40 µm (Hegman ≥ 4); let down with remaining solvent.

- In-process gates per batch: fineness of grind (D1210), Stormer viscosity (D562, target window set at bench), density (D1475, ±0.02 g/mL of theory), nonvolatile content (D2369, ±1% of theory). Density and NV against engine theory are the fastest early indicators of a mischarge.

## 8.2 Qualification testing (MIL-DTL-24441-class)

- Mixed-paint properties: pot life at 73°F/50% RH (viscosity doubling or 25 KU rise); VOC by EPA Method 24; volume solids by D2697; weight/gal by D1475; sheen by D523 (60°, low-sheen target); DFT per SSPC-PA 2 using D7091 gauges.

- Film performance on SSPC-SP 10 near-white blasted steel, 2.5–3.5 mil profile: pull-off adhesion (D4541, target ≥ 500 psi as a working acceptance floor); salt-fog resistance (B117, scribed, 1,000 h screening / 3,000 h qualification, creep and blistering per D1654/D714); seawater immersion (D870 or synthetic-seawater equivalent, 30/90-day inspections); dry-to-touch and recoat windows (D5895 plus practical recoat adhesion at 6 h); low-temperature and 95°F/85% RH application-limit checks.

- Stability: heat-age both components 4 weeks at 120°F (accelerated proxy) with viscosity, settling (D869), and re-test of mixed properties; real-time 36-month program initiated in parallel.

- Data return: each batch and test result is logged as an Amphora experiment/measurement against AMP-EP-0001 or its cloned variant records, giving the customer the structured data-capture the charter requires and feeding the optimization loop.

# 9. Assumptions, Confidence, and Known Gaps

| Item | Confidence | Basis / required verification |
| --- | --- | --- |
| Envelope-constraint compliance (VS, VOC, lb/gal, DFT, coverage, PVC) | High | Deterministic physics from composition; verify with D2697, Method 24, D1475 on first bench batch. |
| Raw-material constants (ρ, NV, EEW, AV, oil absorption) | Medium | Typical published supplier values; replace with lot CoA data before the pilot batch. |
| Polyamide AHEW ≈ 115 → 0.98:1 stoichiometry | Medium | AHEW varies by grade/lot; recompute from CoA; V3/V4 bracket ±5%. |
| Pot life ≥1.5 h, recoat ~6 h, cure profile | Medium | Standard behavior for this resin/curative class at these levels; bench-verify per 8.2. |
| Low-sheen target at PVC 10.3% with 3.9% flatting silica | Medium-Low | Sheen is dispersion- and film-formation-dependent; V5 provides the adjustment path. |
| Additive selection (dispersant, defoamer) at 0.5/0.4 wt% | Medium-Low | Grades intentionally generic pending supplier screening; carriers must be charged against the 42 g/L VOC margin. |
| 36-month shelf life | Low | No accelerated data yet; heat-age program in 8.2 is the screen, real-time study is the proof. |
| Immersion performance vs MIL-DTL-24441-class requirements | Medium | Chemistry and PVC/CPVC position are the canonical route; B117/immersion data are the arbiter. |

# 10. Regulatory, EHS, and Sourcing Notes

VOC: at 298 g/L the system clears the 340 g/L envelope ceiling and typical industrial-maintenance limits, but state/district rules vary (e.g., some CARB districts set 250 g/L for IM coatings); confirm the application jurisdictions before final release. All listed raw materials are established TSCA-inventory industrial chemicals available from multiple U.S. or TAA-country producers, supporting the charter’s domestic-sourcing preference; none is single-source. EHS: xylene and n-butanol are flammable (NFPA 30 storage, Class IC); polyamides and epoxies are dermal sensitizers — closed transfer, grounding/bonding, LEV at the disperser, and standard epoxy-handling PPE are required facility controls. No ITAR implication is identified for this coating class.

# 11. Discovery Annex (Quarantined)

Outside the compliant primary solution, two directions surfaced during design that merit evaluation as future programs: (1) a high-solids variant using a lower-viscosity modified DGEBA plus reactive diluent that the engine projects could reach ~72% volume solids at <250 g/L VOC, trading pot life; and (2) phenalkamide/phenalkamine curatives, which would extend the application window below the envelope’s 65°F floor and shorten recoat, at some cost in color stability. Neither is substituted into AMP-EP-0001.

# 12. References

- Jepson Technical Envelope — Epoxy-Polyamide Marine Hull Primer (customer document, this program’s binding constraint set).

- Self-Directed Formulation & Manufacturing Charter, v1 (customer document).

- MIL-DTL-24441 — Paint, Epoxy-Polyamide (performance-class reference for qualification).

- EPA Method 24 — Determination of Volatile Matter Content of Surface Coatings (40 CFR Part 60, App. A).

- ASTM D2697 (volume solids); D1475 (density); D562 (Stormer viscosity); D1210 (fineness of grind); D2369 (nonvolatile); D523 (specular gloss); D4541 (pull-off adhesion); D7091 & SSPC-PA 2 (DFT); B117 (salt fog); D1654/D714 (corrosion/blistering evaluation); D870 (water immersion); D869 (settling); D5895 (drying times).

- SSPC-SP 10 / NACE No. 2 — Near-White Metal Blast Cleaning.

- Supplier technical literature for the named material classes (DGEBA EEW 182–192 liquid epoxies; polyamides AV 230–246): typical-property values used pending certificates of analysis.

- Amphora platform, formulation record AMP-EP-0001 and variant previews V0–V5 (computation log, July 5, 2026).

This document is a computational design deliverable. Predicted values are model outputs from declared raw-material properties and must be confirmed by the bench program in Section 8 before any production or procurement decision.