# Self-Directed Formulation & Manufacturing Charter

### Marine Hull Primer Program — Companion to Attached Technical Envelope

Customer: A top U.S. Navy prime (masked) Artifact class: Engine charter (objectives + constraints only — not a formulation instruction) Seed inputs: This charter + the attached technical envelope. Nothing else. Version: v1 (template-first; the envelope block is swappable for future partner programs)

## 1. Mandate

The engine receives the attached technical envelope as its sole problem statement and must return a complete, auditable, manufacturable formulation-and-process blueprint that satisfies every requirement in that envelope. The blueprint is a handoff package: it must be directly executable by a contract research organization (CRO) or wet-lab to formulate, synthesize, and test the system in the real world — and the empirical results returned from that bench work feed back to fine-tune the engine, closing the loop between prediction and physical validation. The engine conducts its own exhaustive research — mastering coatings/polymer science, every line of the envelope, and the adjacent fields the envelope implies — and selects or constructs its own methods, models, datasets, and tools to do so. No prior formulations, candidate materials, internal datasets, or human-preferred models are supplied. This document provides objectives and guardrails only; the how is the engine's to discover.

## 2. Operating Principle — Zero Prior, Self-Directed

The engine is to proceed as if approaching this class of problem for the first time. It must:

- Derive the problem space from first principles plus the open literature, rather than from any pre-selected answer.

- Independently determine which model(s), representations, datasets, simulations, and experimental references are appropriate — and construct novel methods of arbitrary sophistication where it judges existing ones insufficient.

- Surface its own assumptions explicitly and treat every choice as a decision it must later justify.

The one binding limit on this freedom (Section 6): however exotic the internal machinery, the delivered recipe must be rendered human-interpretable, fully cited, reproducible, and lab-testable. Novelty in method is unbounded; opacity in the deliverable is not permitted.

## 3. Degrees of Freedom

- Method — unbounded. Full latitude over approach, models, data, and tooling.

- Primary deliverable — bounded. Must conform exactly to the fixed envelope (Section 4) and meet all performance targets (Section 5).

- Discovery — encouraged, quarantined. Superior chemistries, alternative feedstocks, or adjacent coating systems the engine finds along the way are valuable and must be reported — but in the Discovery Annex (Section 8), never substituted into the compliant primary solution.

## 4. Fixed Constraints (binding — the recipe must satisfy all)

- Two-component epoxy-polyamide chemistry

- Nominal 1:1 mix ratio by volume

- Solvent-borne system

- Volume solids ~65% (±2%)

- VOC ≤340 g/L (EPA Method 24 equivalent)

- Dry film thickness ~4.5–6.0 mils per coat

- Recoat window ~6 hours

- Shelf life ~36 months unopened

Open for optimization (variable parameters): manufacturing process sequence; dispersion and mixing strategy; equipment configuration; rheological control; QC methodology.

## 5. Performance Envelope (the recipe must achieve)

Immersion-service protection of exterior carbon steel in marine/saltwater environments; airless spray, brush, or roller application; low sheen; black and yellow (pigmentation non-functional, for identification/visibility only). Mixed-system targets: WFT ~7.0–9.0 mils; coverage ~175–230 ft²/gal; ~9.1 lb/gal; induction ~30 min; pot life ≥1.5 h at 73°F/50% RH; dry-to-touch ~2 h; functional cure ~6 h. Application limits: air/surface ~65–95°F, material ≥60°F, RH ≤85%. Surface prep reference: near-white abrasive blast, 2.5–3.5 mil profile. Storage indoors, 65–95°F.

## 6. Auditability (non-negotiable)

Every element of the deliverable must be:

- Cited — each material choice, parameter, and claim traceable to a source or to an explicitly stated, testable rationale.

- CRO-executable — a contract lab or wet-lab chemist must be able to follow the recipe and process exactly as written and arrive at the same result, without reverse-engineering intent or filling gaps.

- Human-interpretable — reasoning legible to a domain expert; no unexplained outputs.

- Confidence-rated — each recommendation flagged by confidence, with assumptions and known gaps called out.

- Validation-backed — accompanied by a proposed test plan a customer chemist can run to qualify the system against the envelope and against the relevant MIL-DTL-24441-class performance requirements.

## 7. Required Deliverable

The engine determines the full scope; the following is the expected floor, not a ceiling.

- Formulation & BOM — every raw material (resin, curative, solvents, pigments, extenders, additives), its function, target % by weight, key grade/spec attributes, and candidate commercial sources. Both components, mixing/induction behavior, and how the formulation lands the 1:1 / ~65% solids / ≤340 g/L / pot-life targets.

- Manufacturing process — full process flow and sequence, equipment, dispersion/mix parameters, batch sizing, in-line conditioning, and a pilot → production scale-up path with the scale-up risks identified.

- In-process & quality control — viscosity/pot-life control, non-destructive in-process measurements for dispersion/viscosity/cure, early indicators of loss-of-process-control or impending batch failure, batch-record detail, operator-training level, and cross-campaign data-trending practices.

- Supply chain & sourcing — supply sensitivities, single-source risk, lead times, and a domestic-sourcing preference (Buy American / TAA-style) flagged where it bears on the customer.

- Regulatory & EHS — VOC / EPA Method 24, REACH / TSCA, OSHA / NFPA solvent-and-amine handling, applicable state VOC rules, and required facility controls. (ITAR/export-control: note only if clearly implicated; low priority for this program.)

- IP & legal — freedom-to-operate read, relevant patent landscape, and a trade-secret-vs-patent posture recommendation.

- Manufacturability & risk — pinholing/wetting/film-build failure modes, the application-limit parameters most often exceeded in the field and their mitigations, and the environmental variables that most affect manufacturing consistency vs. field performance.

- CRO / wet-lab handoff & feedback loop — the recipe packaged for direct execution by a contract lab, with a proposed formulation-and-test protocol that qualifies the system against the envelope and the relevant MIL-DTL-24441-class performance requirements, plus a structured data-capture template specifying exactly which bench measurements, conditions, deviations, and outcomes the CRO should return — designed so the empirical results flow back to fine-tune the engine on the next iteration.

Seed questions (non-exhaustive — address and exceed): the 15 manufacturing/scale-up/QC questions accompanying the envelope are a starting set, not the boundary. Treat them as the minimum the deliverable must answer and expand beyond them wherever the engine's research identifies gaps the human author did not.

## 8. Discovery Annex (separate, quarantined)

Report — outside the compliant primary solution — any superior epoxy-polyamide variants, alternative chemistries, novel feedstocks, or adjacent high-value coating systems uncovered during research, with enough detail for us to evaluate them as future programs.

## 9. Confidentiality

The customer is referred to throughout as "a top U.S. Navy prime." Outputs default to maskable; the customer's true identity does not appear in any deliverable.

Reuse: for subsequent partner programs (energy, oil & gas, defense, etc.), replace Sections 4–5 with that partner's technical envelope. Sections 1–3 and 6–9 are the standing scaffold.